## Slide 1: Overview
What are P-type and N-type semiconductors?
Intrinsic Semiconductors
Doped Semiconductors
    N-type and P-type Semiconductors
Drift current
Diffusion Current
pn Junction

## Slide 2: What are P-type and N-type ?
Semiconductors are classified into P-type and N-type semiconductor.
P-type: A P-type material is one in which holes are majority carriers i.e. they are positively charged materials (++++)
N-type: A N-type material is one in which electrons are majority carriers i.e. they are negatively charged materials (---)

## Slide 3: Intrinsic Semiconductors
Intrinsic semiconductor : is one which is not doped. (Saf yarıiletken)
  One example is pure silicon.
Generation –is the process of free electrons and holes being created.
Recombination –is the process of free electrons and holes disappearing.
In thermal equilibrium, generation and recombination rates are equal.(Isıl denge, enerji alışverişi yoktur. )

## Slide 4: Conductors and Insulators

## Slide 5: Intrinsic Smiconductors
In thermal equilibrium, the behavior below applies...
  = number of free electrons and holes / unit volume
  p= number of holes
  n= number of free electrons
  =

## Slide 6
Carrier Concentration
Intrinsic Semiconductors (Pure single-crystal material)
For an intrinsic semiconductor, the concentration of electrons (ni) in the conduction band is equal to the concentration of holes (pi) in the valence band.
ni : intrinsic electron concentration
pi : intrinsic hole concentration
ni = pi
ni :intrinsic carrier concentration, which refers to either the intrinsic electron or hole concentration
SI
SI
SI
SI
SI
SI
SI
SI
SI
SI

## Slide 7: Doped Semiconductors

## Slide 8: Electron and Hole Concentrations in n and p type materials
Under thermal equilibrium conditions, the product of the conduction-electron density and the hole density is ALWAYS equal to the square of ni
P-type material
N-type material
Number donor atoms
Number of free electrons in n-type
Number acceptor atoms
ni : The concentration of conduction electrons in intrinsic silicon

## Slide 9: Doped Semiconductor
The concentration of silicon atoms in the crystal is almost 1023/cm3
In typical semiconductor devices, the concentration of impurity atoms in the range from 1015/cm3 to 1019/cm3 atoms.
The fraction of impurity is very small, about 1 part in 106.
  The metallurgical properties of the crystal are not changed perceptibly.
  However, the electrical properties of the crstal are greatly changed by the impurity.

## Slide 10: Electron and Hole Densities
The product of electron and hole densities is ALWAYS equal to the square of intrinsic electron density regardless of doping levels.
Majority Carriers (p type) :
Minority Carriers (p type) :
Majority Carriers (n type) :
Minority Carriers (n type) :

## Slide 11: Doped Semiconductors
Number electrons in n-type
Number donor atoms

## Slide 12: P-type Semiconductors

## Slide 13: Example

## Slide 14: Comparision

## Slide 15: Current Flow in Semiconductors
There are two mechanisms by which holes and electrons move through a crystal:
  Drift Current
  Diffusion Current

## Slide 16: Drift Current

## Slide 17
What type of charges are responsible for current flow in conductors?
What type of charges are responsible for current flow in semiconductors?
  What is mobility µ?
    In solid-state physics, the electron mobility characterizes how quickly an electron can move through a metal or semiconductor, when pulled by an electric field.
Drift current

## Slide 18
Drift Current

## Slide 19
Electrons move with velocity 2.5 times higher than holes
Drift velocity
Drift current

## Slide 20
For doped n type silicon,
For doped p type silicon,
  Unit: mho/cm
  Unit: ohm-cm
Resistivity and Conductivity of Semiconductor

## Slide 22: Resistivity Dependence on Doping

## Slide 23: Diffusion Current

## Slide 24: Second Charge Transportation Mechanism: Diffusion
Charge particles move from a region of high concentration to a region of low concentration. It is analogous to an every day example of an ink droplet in water.

## Slide 25: Current Flow: Diffusion
Diffusion current is proportional to the gradient of charge (dn/dx) along the direction of current flow.
Its total current density consists of both electrons and holes.

## Slide 26: Diffusion Current
The hole density varies depending on the distance
The electron density varies depending on the distance.
Hole direction
Current direction
Electron direction
Current direction

## Slide 27: Einstein Relationship
Magnitude of electron charge
Boltzman constant

## Slide 28: Diffusion Current

## Slide 29: Total Current

## Slide 30
Drift current
Drift current is caused by electric fields
Direction of the drift current is always in the direction of the electric field.
Obeys Ohm’s law:
Diffusion Current
Diffusion current is caused by variation in the carrier concentration
Direction of the diffusion current depends on the gradient of the carrier concentration
Obeys Fick’s law:

## Slide 31: pn junction structure

## Slide 33: Depletion Region
There is a heavy concentration of holes in the p-type region and only a light concentration of holes in the n-type region,
Holes move to from p-type into the n-type region by diffusion and they disappear by recombination very quicky.
PN Junction
Diffusion
Depletion Region

## Slide 34
P-N Junction

## Slide 35: P-N Junction

## Slide 37
Depletion region

## Slide 39: Built-in Potential
Because of the electric field across the junction, there exists a built-in potential. Its derivation is shown above.
Barrier potential
Number donor atoms
Free electrons in intrinsic silicon
diffusion current
drift current
Number acceptor atoms

## Slide 40: Poission equations

## Slide 41
p-n junction
Depletion region should be neutral :
W

## Slide 42: Width of Depletion Region
w
Distances of the depletion region on the p side
Distances of the depletion region on the n side
Total width of depletion region
If impurity density is less, the thickness of the depletion layer is greater.

## Slide 43: Understanding of mobility

## Slide 44: Definition of Resistance